Rezumat

Procesele de piroliză a compuşilor organici lichizi şi gazoşi sunt destul de bine detaliate şi caracterizate în literatură de specialitate. În ceea ce priveşte caracterizarea proceselor de piroliză a materialelor vegetale, aceasta este în plină dezvoltare, deoarece acestea sunt resurse energetice regenerabile, cu un potenţial uriaş de înlocuire a combustibililor fosili.

Cercetările care fac obiectul prezenţei lucrări au urmărit investigarea procesului de piroliză a unor specii de largă abundenţă (boabe de grâu în cazul de faţă), neimpregnate, în prezenţa dioxidului de carbon că gaz purtător. S-a urmărit evidenţierea creşterii randamentului pirolizei în compuşi volatili, şi identificarea posibilităţilor de valorificare a datelor pentru a optimiza procesul. Lucrarea a fost structurată pe şase capitole, cu accent deosebit pe prezentarea rezultatelor cercetărilor proprii.

Cercetarea pirolizei materialului vegetal selectat a fost efectuată conform unui plan experimental de tipul 23 ce a urmărit stabilirea corelaţiilor dintre factorii de proces şi variabilele dependente. Modelarea fenomenologică s-a bazat pe alegerea unui model cinetic global monoreactie şi identificarea parametrilor acestuia. Cercetarea experimentală a materialului vegetal selectat a avut ca principal scop determinarea corelaţiilor dintre factorii procesului şi răspunsurile acestuia pentru a face o optimizare a lui în funcţie de cerinţe. Astfel, s-a urmărit influenţa parametrilor de intrare ai procesului asupra răspunsurilor acestuia pentru a putea obţine maximum din unul din cele trei produse ale procesului şi/sau chiar maximim din cele trei.

Abstract

The pyrolysis processes of the liquid and gaseous organic compounds are very well described and characterized in literature, whereas the pyrolysis of the vegetal materials is continuously improving, considering their great potential to substitute the fossil fuels.

The purpose of this research was to investigate the pyrolysis of some abundant un-impregnated vegetal materials (the wheat grains in this case), when using carbon dioxide as carrier gas. The research was focused both on highlighting the increasing of the volatiles yield and on identifying the possibilities to capitalize the resulting data for process optimization. The thesis consists in 6 chapters focusing especially on revealing the results of the research activity performed by the author.

The investigation of the selected vegetal material pyrolysis was performed according to a factorial experimental plan 23 type in order to achieve a correlation between the process factors and the dependent variables. The process modelling was based on a considered mono-component global kinetic model whose parameters had to be determined. Experimental research of the selected vegetal material had as main purpose to determine the correlation between the process factors and its responses in order to optimize it according to specifications. Thus, the influence of the entry parameters to the responses was determined in order to obtain o maximum of one of the process products and/or of all three of them.