Studiul implicaţiilor copolimerilor funcţionali în obţinerea materialelor nanostructurate

Rezumat

Teza de doctorat are ca scop principal obţinerea de materiale nanostructurate pornind de la diferiţi copolimeri funcţionali ai anhidridei maleice. S-au studiat reacţiile anhidridei maleice (MA) cu monomeri cum ar fi divinil-benzenul (DVB), stirenul, acetatul de vinil, stiren sulfonat de sodiu, butil vinil eter, etc.

Pentru mulţi polimeri, cât şi pentru copolimerii MA, adiţia de agenţi de ranforsare nano-fazici cum ar fi montmorilonitul (MMT) poate duce la îmbunătăţirea unor proprietăţi. S-a încercat încapsularea unor derivaţi ai sodiu montmorilonitului modificat, cu trimetiletoxisilan, vinildimetiletoxisilan, fenildimetiletoxisilan, octildimetilmetoxisilan, octadecildimetilmetoxisilan, în particulele de polimer obţinute prin copolimerizarea în dispersie a DVB cu MA.

Un alt obiectiv al acestei teze a fost prepararea particulelor hibride prin procesul sol-gel al tetraetoxisilanului împreună cu metacriloxipropiltrimetoxisilanul sau din copolimeri alternanţi viniltrietoxisilan-anhidridă maleică.

Prin generarea în sistem a nanoparticulelor de Ag° din reacţia AgNO3 şi NaBH4 în mediu apos s-au obţinut nanocompozite de copolimeri DVB-MA.

Se mai studiază formarea nanoparticulelor de Ag° în soluţii de polielectroliţi de concentraţii diferite. Drept polielectroliţi au fost utilizaţi copolimeri alternanţi ai MA cu acetat de vinil şi 4-stirensulfonatul (StSO3Na) dispersaţi în apă cu săruri de sodiu.

O ultimă direcţie a fost obţinerea şi caracterizarea de nanocompozite cu proprietăţi magnetice care să permită încapsularea unui vector magnetic.

Study on functional copolymers involvement for nanostructural materials obtaining

Abstract

The PhD thesis has as main purpose the obtaining of nanostructured materials using various functional copolymers of maleic anhydride. Maleic anhydride (MA) reactions with monomers as divinylbenzene (DVB), sodium styrene sulphonate, butyl vinyl ether, etc were studied.

For many polymers, as well as for MA copolymers, reinforcement agents’ adition with nano dimensions as montmorillonit (MMT), can improve the final properties. We encapsulate derivatives of sodium montmorillonites layered silicates with trimethoxysilane, vinyldimethylethoxysilane, phenyldimethylethoxysilane, octyldimethylmethoxysilane, octadecyldimethylmethoxysilane, in polymer particles synthesized through dispersion copolymerization of DVB with MA.

Another goal of this thesis was to obtain hybrid particles through sol-gel process of tetraethoxysilane with metacryloxypropyltrimethoxysilane or from alternating copolymers vinyltriethoxysilane-maleic anhydride. 	Furthermore, we obtained nanocomposites based on DVB-MA copolymers with Ag° nanoparticles, previously generated in aqueous medium through the reaction of AgNO3 with NaBH4.

We also studied Ag° nanoparticles obtaining in polyelectrolytes solutions of different concentrations. We used as polyelectrolytes alternating copolymers of MA with vinyl acetate and 4 –sodium styrene sulphonate dispersed in water with sodium salts.

The last direction was the obtaining and characterization of nanocomposites with magnetic properties able to encapsulate magnetic vector.